## Slide 1: Machine learning denoising of high-resolution nanotomography data
P05 nanotomography at PETRA III, DESY
Silja Flenner
Institute for Materials Research
Helmholtz AI 2024

## Slide 2: Full-field nanotomography @ P05, PETRA III, DESY
Camera
FZP
Sample
OSA
Beamstop
f = 133 mm
z1 = 50 mm – 3000 mm
z2 = 16 m – 22 m
Camera
Beamshaper
Sample
OSA
Beamstop
790 mm
50 mm – 100 mm
20 m – 22 m
FZP
Nanotomography:
Resolution < 50 nm
Standard scans 15 min
Fast scanning
In situ applications
Holotomography
48 nm - 37 nm lines
Absorption
Zernike Phase contrast
1 µm
1 µm
Flenner et al. Journal of Synchrotron Radiation, (2020)
Flenner et al. Optics Express (2020)
Transmission X-ray Microscopy

## Slide 3: Machine learning for high time resolution
Flenner et al. (2020), Journal of Synchrotron Radiation
Pelt & Sethian (2017), Proc. of the Nat. Ac. of Sc. of the United States of America
https://github.com/dmpelt/msdnet
15 min
3 min
36 s
6 s
1 h
Nanoporous gold
3D test pattern for Nanotomography

## Slide 4: Machine learning for high time resolution
Machine learning (ML) for very short scan times
Input
Reference
Train network
Flenner et al. (2020), Journal of Synchrotron Radiation
Pelt & Sethian (2017), Proc. of the Nat. Ac. of Sc. of the United States of America
6 s + ML
Output
https://github.com/dmpelt/msdnet
15 min
3 min
36 s
6 s
1 h

## Slide 5: Machine learning denoising: Noise2Inverse
Input
Target
ML
Trained network
Stack of projections
reconstruct
train
apply
2 stack with ½ projections
2 reconstructed stacks
split
Hendriksen et al. (2020). IEEE Transactions on Computational Imaging
Flenner et al. (2022) Journal of Synchrotron Radiation
https://github.com/dmpelt/msdnet

## Slide 6: Denoising of standard scans
Applicable on standard scans without reference scan
Multi-scale dense network (msdnet)
5 input channels (5 slices, 2.5D training)
Image size: 1024 x 1024
Training data size: 100 – 300 slices
Test data size: 40 – 80 slices
x-y view
y-z view
Unfiltered
Flenner et al. (2022) Journal of Synchrotron Radiation
Hendriksen et al. (2020). IEEE Transactions on Computational Imaging
ML filter
3 µm
3 µm
3 µm
3 µm
https://github.com/dmpelt/msdnet
Notes: Recorded 2000 projections

## Slide 7: Applicability
3D Human Bone Anatomy
Stockhausen et al. ACS Nano, 15 (1), 455-467, 2021
Original
Trained on same sample
Trained on similar sample
Training is the most time consuming step (up to several hours)
Typical TXM experiment:
Batch of similar samples
In collaboration with Prof. B. Busse (UKE)

## Slide 8: Machine learning denoising
Input
Target
ML
Trained network
Stack of projections
reconstruct
train
apply
2 stack with ½ projections
2 recostructed stacks
split
6 min
3 min
Network is trained to be applied on a scan with half the number of projections!

## Slide 9: Decreasing scan time for in situ experiments
3D Human Bone Anatomy
6 min
3 min
3 min – ML filtered
Trained network
training

## Slide 10: The next step: Dual-beam tomography for ML
left & right
interlaced
left
input
right
target
ML
result
Flenner et al. (2024) Journal of Synchrotron Radiation

## Slide 11: Summary
Machine learning denoising
    Very short scans (with high quality reference scan)
    Standard scans without a reference scan
    Helps to reduce scan time for in situ experiments
    Dual- beam setup for artifact removal
silja.flenner@hereon.de, imke.greving@hereon.de

## Slide 12: Thank you
Silja Flenner
silja.flenner@hereon.de, imke.greving@hereon.de
Johannes Hagemann
Felix Wittwer
André Rothkirch
Adam Kubec
Peng Qui
Florian Döring
Christian David
Hereon Team
Imke Greving
Stefan Bruns
Elena Longo
Malte Storm
Berit Zeller-Plumhoff
Felix Beckmann
Fabian Wilde
Jörg Hammel
Julian Moosmann
Jens Breling
Hilmar Burmester
Ursula Tietze
Christina Krywka
Martin Müller
Samples
Kilian Stockhausen (UKE)
Björn Busse (UKE)
Andrew J. Parnell
(University of Sheffield)
Erica Lilleodden (hereon)